**Requirement Specification Textile Boot Bag**

1. **Requirements**

**1.1. Description of the requirement**

The Danish Ministry of Defence, Acquisition and Logistics Organisation (DALO) wants to acquire 4.000 Textile Boot Bags for transporting muddy boots in a backpack. The Textile Boot Bag is a simple PU coated polyamide bag with drawstring closure. The Textile Boot Bag secondarily functions as a sleeping bag protection covering the soldier’s boots, when he/she sleeps with boots on.

The Textile Boot Bag will be used by men and women for both training and actual military operations. The Textile Boot Bag must therefore be easy to use, durable have a matte earthly green or brown colour in order to provide some camouflage in various terrains.

**1.2. Description and definitions**

The requirement specification, cf. section 1.4, describes all the requirements for the acquisition and consists of six columns with the following information:

|  |  |
| --- | --- |
| "#" | ID number |
| "Requirement" | Requirement description |
| "Classification" | The classification of the requirement as further described in section 1.3 |
| "DALO remarks" | Further information regarding the requirement |
| "Requirement compliance" | The tenderer's indication of compliance (YES or NO) |
| "Tender description" | Requirements regarding the tenderer's compliance description |

**1.3. Classification**

All requirements are mandatory requirements (SHALL) and shall be fulfilled by the tenderer. If just one of the mandatory requirements is not fulfilled, the tenderer's tender will not be taken into further consideration.

**1.4. Requirement and response sheet**

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| **#** | **Requirement** | **Classification** | **DALO remarks** | **To be filled out be the tenderer** | | | |
| **Requirement compliance**  **(tick a box)** | | | **Tenderer's description** |
| **YES** | **NO** | |
| **1** | The Textile Boot Bag shall fulfill the requirements in Appendix 1 (TT35201) | SHALL |  |  |  | |  |
| **2** | The Textile Boot Bag shall be made of 250 - 300 dtex 1/1 plain weave polyamide 6.6. | SHALL |  |  |  | |  |
| **3** | The polyamide fabric shall have a durable PU coating of 30 - 40 g/m2 on the back side of the fabric. | SHALL |  |  |  | |  |
| **5** | The Textile Boot Bag shall withstand the severe wear and tear that is expected form the daily use in operative tasks. All materials including trimmings (cord lock, grommets and draw cord) and sewing thread as well as craftsmanship shall therefore be to a high industry standard and should not rust or tenderize*.* | SHALL | The offer will be tested by DALO. The test includes but is not limited to the following key points which the boot bag shall withstand without failure in order to pass the test.   * Operating/sliding the cord lock 50 times by hand force. * Pulling the boot bag in several directions to simulate foot movement in sleeping bag to test the stitching. * Pulling the grommets and drawstring by hand force. |  | |  |  |
| **7** | The terms of delivery shall be INCOTERMS 2020 DAP Hjørring, Denmark. | SHALL |  |  |  | |  |
| **8** | The delivery shall be of 4.000 Textile Boot Bags | SHALL |  |  |  | |  |
| **9** | The colour of the Textile Boot Bag shall be earthly green or earthly brown. | SHALL | There are no colour code available |  |  | |  |
| **10** | The delivery time shall be maximum 120 calendar days from order placement. | SHALL |  |  |  | |  |